SECTION 06400

TITLE: Architectural Millwork

FUTRUS Solid Surface Cabinet Doors

Display hidden notes to specifier by using File/Options/Display/Hidden Text

Futrus Solutions – solid surface products

This section is based on products by Futrus, which is located at:

154 Distl Avenue

Mansfield, OH 44902

Toll Free: 877-388-7871

Fax: 410-526-1009

Web: www.futrus.com

E-mail: info@futrus.com
 
Futrus is the leading manufacturer of solid surface cabinet doors.  All products are manufactured to the specifier's requirements.  Futrus’ primary manufacturing facility is in Mansfield, OH and ships product throughout North America & Canada.

- GENERAL

  - SECTION INCLUDES

A.  FUTRUS Solid Surface Cabinet Doors

  - RELATED SECTIONS

* NOTE TO SPECIFIER* Delete any sections below not relevant to this project; add others as required

A. Section 06410 – Custom Cabinets

B. Section 12320 – Manufactured Wood Casework

C. Section 12350 – Specialty Casework

  - DEFINITIONS

    - Solid-surface: Nonporous, homogeneous material maintaining the same composition throughout the part with a composition of acrylic polymer, aluminum trihydrate filler and pigment.

  - SUBMITTALS

    - Submit under provisions of Section 01300

    - Manufacturer’s data sheets on product being used.

  - QUALITY ASSURANCE

    - Installer qualifications: Manufacturer’s authorized representative who is trained and approved for installation of units required for this Project.

B. Source Limitations:  Obtain solid-surface modular casework through one source from a single manufacturer.

C. Manufacturer Qualifications:

1.Provider of fabricator and installer training.

2.Shop that employs skilled workers who custom fabricate and thermoform products similar to those required for this project and whose products have a record of successful in-service performance.

D. Applicable standards:

1.	Standards of the following, as referenced herein:

A.	American National Standards Institute (ANSI)

B.	American Society for Testing and Materials (ASTM)

C.	National Electrical Manufacturers Association (NEMA)

D.	NSF International

2.	Fire test response characteristics:

A.	Provide with the following Class A (Class I) surface burning characteristics as determined by testing identical products per UL 723 (ASTM E84) or another testing and inspecting agency acceptable to authorities having jurisdiction:

1)	Flame Spread Index: 25 or less.

2)	Smoke Developed Index: 450 or less.

  - DELIVERY, STORAGE, AND HANDLING

    - Store products in manufacturer’s unopened packaging until ready for installation.

    - Store in dry, protected, well ventilated area and protect from damage

    - Store products in an enclosed area protected from moisture and heat. Maintain a consistent temperature and humidity Store products in manufacturer's unopened packaging until ready for installation.

    - If solid-surface doors must be stored in other than installation areas, store only in areas where environmental conditions comply with requirements specified in "Project Conditions" Article.

    - Keep finished surfaces protected during handling and installation with protective covering of polyethylene film or other protective covering during handling and installation. Refer to CLEANING AND PROTECTION in Part 3 of this section

  - PROJECT CONDITIONS

    - Environmental Limitations:  Do not deliver or install manufactured solid surface casework until spaces are enclosed and weather-tight, wet work in spaces is complete and dry, work above ceilings is complete, and temporary HVAC system is operating and maintaining ambient temperature and humidity conditions at occupancy levels during the remainder of the construction period.

  - COORDINATION

    - Coordinate sizes and locations of framing, blocking, furring, reinforcements, and other related units of work specified on other Sections to ensure that solid-surface modular casework system can be supported and installed as indicated.

  - WARRANTY

A.	Special Warranty:  Manufacturer's standard form in which manufacturer agrees to repair or replace solid-surface modular casework components that fail in materials or workmanship within specified warranty period.

1.	Warranty Period:  Five years from date of Substantial Completion.

2.	Warranties do not apply in the event of neglect or abuse or the unit or parts involved.

- PRODUCTS

  - MANUFACTURERS

A.  	Acceptable Manufacturer:

Futrus® Solutions with Corian® Design

154 Distl Ave, Mansfield, Ohio 44902

Phone 1.877.FUTRUS1(388.7871)

Fax 419.526.1009 | Website www.futrus.com

B.	Basis-of-Design Product:  Subject to compliance with requirements, provide Futrus® Solutions solid-surface door system.

** NOTE TO SPECIFIER **  Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

B.	Substitutions:  Not permitted.

C.	Requests for substitutions will be considered in accordance with provisions of Section 01600.

  - MATERIALS

    - Solid-surfacing Material:  Provide solid-surface DOORS/DRAWERS made with Corian®

          - Solid polymer components:

A. Cast, nonporous, filled polymer, not coated, laminated or of composite construction with through body colors meeting ANSI Z124.3 or ANSI Z124.6, having minimum physical and performance properties specified.

B. Superficial damage to a depth of 0.010 inch (.25 mm) shall be repairable by sanding and/or polishing.

C. Performance characteristics:  Physical properties data sheet is available upon request from Futrus® Solutions with Corian®

          - Color:  As selected from manufacturer’s full range.

          - Finish:  Manufacturer’s standard matte finish.

PART 3   	 EXECUTION

  - EXAMINATION

A.	Examine areas, with Installer present, for compliance with requirements for installation tolerances, location of reinforcements, and other conditions affecting performance of solid-surface modular casework.

1.	Do not begin installation until substrates have been properly prepared.

2.	Proceed with installation only after unsatisfactory conditions have been corrected.

3.2      INSTALLATION

- Install in accordance to manufacturer’s instructions

- Install hardware uniformly and precisely. Set hinges snug and flat in mortises unless otherwise indicated. Adjust and align hardware so moving parts operate freely and contact points meet accurately. Allow for final adjustment after installation.

- Adjust solid-surface modular casework and hardware so doors and drawers align and operate smoothly without warp or bind and contact points meet accurately.  Lubricate operating hardware as recommended by manufacturer.

3.3	PROTECTION

A. 	 Protect installed product until completion of project.

END OF SECTION